# Technical Specification: Flash Butt Welding of Rails

Specification No.: ENGG/TS/WELD/2026/05     Issue Date: 20 September 2026     Status: Draft for review

# 1. Introduction

This specification covers the requirements for flash butt welding (FBW) of 60 kg/m, 90 UTS rails to form long welded rail (LWR) panels at a fixed welding plant. It defines materials, equipment, process parameters, inspection, and acceptance criteria.

# 2. Referenced Standards

- IRS T-12: Rails (60 kg/m, 90 UTS) - material specification

- IRS T-59: Flash butt welding of rails

- EN 14587-1: Railway applications - Track - Flash butt welding of new rails

- IRPWM: Indian Railways Permanent Way Manual

# 3. Materials

## 3.1 Rail Chemical Composition

| Element | Minimum (%) | Maximum (%) |
| --- | --- | --- |
| Carbon (C) | 0.60 | 0.80 |
| Manganese (Mn) | 0.80 | 1.30 |
| Silicon (Si) | 0.10 | 0.50 |
| Phosphorus (P) | - | 0.030 |
| Sulphur (S) | - | 0.030 |
| Hydrogen (H) | - | 2.5 ppm |

## 3.2 Mechanical Properties

| Property | Requirement |
| --- | --- |
| Tensile strength | Minimum 880 MPa (90 UTS grade) |
| Elongation | Minimum 10% |
| Hardness (head) | 260 - 300 HB |
| Fatigue (2 x 10^6 cycles) | No failure at stress range 240 MPa |

# 4. Equipment

Welding shall be performed on a stationary flash butt welding machine with the following minimum capability:

| Parameter | Value |
| --- | --- |
| Maximum upset force | 1000 kN |
| Rated power | 250 kVA |
| Control | Microprocessor, programmable, with data logging |
| Rail straightness correction | Hydraulic, +/- 0.3 mm over 1 m |
| Weld trimming | Hot shearing within 90 s after upset |

# 5. Welding Process Parameters

| Stage | Parameter | Typical Value | Tolerance |
| --- | --- | --- | --- |
| Preheating | Number of pulses | 12 | +/- 2 |
| Flashing | Flash duration | 55 s | +/- 5 s |
| Flashing | Burn-off length | 12 mm | +/- 1 mm |
| Upsetting | Upset current time | 1.6 s | +/- 0.2 s |
| Upsetting | Upset length | 5 mm | +/- 1 mm |
| Post-weld | Normalising temperature | 850 C | +/- 25 C |

# 6. Inspection and Testing

## 6.1 Visual and Geometric

- Straight-edge test (1 m): vertical deviation 0 to +0.3 mm on the running table.

- Lateral deviation of gauge face not to exceed 0.3 mm over 1 m.

- No visible cracks, notches or burn marks on the weld collar.

## 6.2 Non-destructive and Destructive Tests

| Test | Frequency | Acceptance Criterion |
| --- | --- | --- |
| Ultrasonic testing | 100% of welds | No indication above reference level - 6 dB |
| Slow bend test | 1 per 100 welds | Fracture load not less than 1450 kN, deflection not less than 18 mm |
| Macro-etch | 1 per 500 welds | No lack of fusion or inclusions |
| Hardness traverse | 1 per 500 welds | Within 20 HB of parent rail |

# 7. Documentation

Each weld shall carry a unique identification marked on the web, comprising welding plant code, date, machine number and serial number. Machine data logs shall be retained for the service life of the rail panel.

# 8. Non-Conformance

Any weld failing a prescribed test shall be cut out and rejected. Where a failure is found in a sample test, all welds produced since the last satisfactory test shall be 100% re-tested.